| INSPECTION & TEST PLAN |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CLIENT |  | ENER TECHNOLOGY |  |  | ITP NO : TBA Rev. 00 |  |  |  |  |  |  |  |  | DATE : 04.09.2024. |  |  |  |  |  |
| PROJECT |  | TBA |  |  | JOB TITLE | REFRIGERATION SKID PACKAGE |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P.O.No & Date |  | TBA |  |  | SKID GA. DRG. NO. | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |
| W.O.NO |  | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| VENDOR |  | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CLIENT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| SL NO | QUALITY RELATED ACTIVITY |  | REFERENCE | CHARACTERISTICS TO | ACCEPTANCE |  | VERIFYING | AGENCY |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | DOCUMENTS | BE VERIFIED | STANDARD |  | DOCUMENTS | VENDOR |  | ENER |  |  |  |  |  |  |  | REMARKS |  |
|  | INSPECTION & TEST PLAN (FOR PIPING) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1.0 | ENGINEERING DOCUMENTATION & DRAWING |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1.1 | Review fabricaton drawing |  | Conformance to B31.3, Clent Spec. | Drawings | ASME B 31.3, Clent Spec |  | Project Documents. | H |  | R |  |  |  |  |  |  |  |  |  |
| 1.2 | Welding Procedures & Procedure Qualification Records & Welding Repair Procedure |  | ASME Sec IX, ASME B31.3, Client Spec. | Approved WPS / PQR | ASME Sec IX ,Client Spec. |  | WPS / PQR | H |  | R |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | H |  | R |  |  |  |  |  |  |  |  |  |
| 1.3 | Welder's Performance Qualification Records |  | ASME Sec IX, Client Spec. | Approved WPQR | ASME Sec IX, Client Spec. |  | WPQR | H |  | R |  |  |  |  |  |  |  |  |  |
| 1.4 | NDE Procedures (RT , MT & PT), Hardness test procedure |  | ASME Sec V / Client Spec. | NDE Procedures, Hardness test procedure | ASME SEC V / Client Spec. |  | NDE Procedures, Hardness test procedure | H |  | R |  |  |  |  |  |  |  |  |  |
| 1.5 | NDE Operator Qualification |  | ASME Sec V / Client Spec. | Qualification & Renewal of operators. | ASNT-SNT-TC-1A , Client Spec. |  | Certificates | H |  | R |  |  |  |  |  |  |  |  |  |
| 1.6 | Visual Inspection procedure |  | Conformance to B31.3, Client Spec. | Visual Inspection procedure | Approved Drg - ASME B 31.3, Client Spec. |  | Visual Inspection procedure | H |  | R |  |  |  |  |  |  |  |  |  |
| 1.7 | PMI Procedure |  | Approved drawing & ASME Sec II Part A | Elements to be confirmed | As per approved drawing & ASME Sec II Part A |  | PMI Procedure | H |  | R |  |  |  |  |  |  |  |  |  |
| 1.8 | Hydro Test Procedure |  | Conformance to B31.3, Client Spec. | Pressure Testing of process piping | Approved Drg - ASME B 31.3, Client Spec. |  | Hydro Test Procedures | H |  | R |  |  |  |  |  |  |  |  |  |
| 1.9 | Pickling & Passivation Procedure |  | ASTM A380 | Pickling & Passivation Procedure | As per approved procedure, ASTM A380 |  | Pickling & Passivation Procedure | H |  | R |  |  |  |  |  |  |  |  |  |

| INSPECTION & TEST PLAN |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CLIENT |  | ENER TECHNOLOGY |  |  | ITP NO : TBA Rev. 00 |  |  |  |  |  |  |  |  | DATE : 04.09.2024. |  |  |  |  |  |
| PROJECT |  | TBA |  |  | JOB TITLE | REFRIGERATION SKID PACKAGE |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P.O.No & Date |  | TBA |  |  | SKID GA. DRG. NO. | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |
| W.O.NO |  | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| VENDOR |  | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CLIENT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| SL NO | QUALITY RELATED ACTIVITY |  | REFERENCE | CHARACTERISTICS TO | ACCEPTANCE |  | VERIFYING | AGENCY |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | DOCUMENTS | BE VERIFIED | STANDARD |  | DOCUMENTS | VENDOR |  | ENER |  |  |  |  |  |  |  | REMARKS |  |
| 1.10 | Painting Procedure |  | As per approved procedure | Painting Procedure | As per approved procedure |  | Painting Procedure | H |  | R |  |  |  |  |  |  |  |  |  |
| 2.0 | MATERIAL PREPARATION & PRE FABRICATION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2.1 | Material Test Certificates |  | ASME Sec II Part - A. | Chemical & Mechanical Properties , Markings, Minimum Thk and Surface Conditions. | As per Approved Drawing in accordane with ASME Sec II Part - A. |  | MTC & Inspection Report. | H |  | R |  |  |  |  |  |  |  |  |  |
| 2.2 | Visual & dimensional of raw material |  | ASME Sec II Part - A. | Visual & dimensional inspection | As per Approved Drawing in accordane with ASME Sec II Part - A. |  | MTC & Inspection Report. | H |  | SW |  |  |  |  |  |  |  |  |  |
| 2.3 | PMI for Stainless steel materials |  | Approved Drawings | Elements to be verified as per approved procedure | Approved Procedure |  | PMI Report | H |  | SW |  |  |  |  |  |  |  |  |  |
| 3.0 | FABRICATION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3.1 | Internal Cleaning |  | Approved Procedure | Visual | Approved Procedure |  | Inspection Report. | H |  | SW |  |  |  |  |  |  |  |  |  |
| 3.2 | Length Marking, Cutting |  | Approved Drawing | Approved Drawing , Length , Profile Cutting of plates dimensions and marking. | Approved Drawing |  | … | H |  | SW |  |  |  |  |  |  |  |  |  |
| 3.3 | Material Traceability |  | Approved Drawing | Heat Number & Specification | Approved Drawing |  | Inspection Report. | H |  | SW |  |  |  |  |  |  |  |  |  |
| 3.4 | Preparation of Piping with Attachments |  | Approved Drawing | Approved Drawing & Dimensions | Approved Drawing |  | … | H |  | SW |  |  |  |  |  |  |  |  |  |
| 3.5 | Pipe with flanges Attachments fitup |  | Approved Drawing | Parellality, Perpendicularity Orientation, Dimensions& Alignment | Approved Drawing |  | … | H |  | SW |  |  |  |  |  |  |  |  |  |
| 4.0 | VISUAL INSPECTION OF WELD |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4.1 | WELDING & VISUAL INSPECTION |  | Approved Weld Visual Procedure ; Approved WPS | WELD SIZE. & Appearance | Approved Drawing & ASME B 31.3 Table 341.3.2 |  | Inspection Report. | H |  | SW |  |  |  |  |  |  |  |  |  |
| 5.0 | NDE |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

| INSPECTION & TEST PLAN |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CLIENT |  | ENER TECHNOLOGY |  |  | ITP NO : TBA Rev. 00 |  |  |  |  |  |  |  |  | DATE : 04.09.2024. |  |  |  |  |  |
| PROJECT |  | TBA |  |  | JOB TITLE | REFRIGERATION SKID PACKAGE |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P.O.No & Date |  | TBA |  |  | SKID GA. DRG. NO. | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |
| W.O.NO |  | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| VENDOR |  | TBA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CLIENT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| SL NO | QUALITY RELATED ACTIVITY |  | REFERENCE | CHARACTERISTICS TO | ACCEPTANCE |  | VERIFYING | AGENCY |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | DOCUMENTS | BE VERIFIED | STANDARD |  | DOCUMENTS | VENDOR |  | ENER |  |  |  |  |  |  |  | REMARKS |  |
| 5.1 | 15 % RT On Butt welds 15 % MT / PT On other Wellds. |  | Approved RT, PT, MT procedure, | Weld Soundness & Quality | Approved Drawing & ASME B 31.3 Table 341.3.2, 344.4.2, 344.3.2 |  | RT,MT,PT REPORTS | H |  | R |  |  |  |  |  |  |  |  |  |
| 6.0 | Final Inspection (Before Hydro) |  | ASME B31.3, Approved Drawing, | Visual , Dimension & Orientation | Approved Drawing & ASME B 31.3 |  | Inspection Report. | H |  | H |  |  |  |  |  |  |  |  |  |
| 7.0 | Hydro test . |  | ASME B31.3, Approved Drawing, | Pressure & Holding Time | Approved Drawing & ASME B 31.3 Sec.345.4 & As per approved procedure |  | pressure Chart &Inspection Report. | H |  | H |  |  |  |  |  |  |  |  |  |
| 8.0 | Pickling / Passivation on Stainless Steel & SDSS Pipe Spools (External Surface Only) |  | ASTM A380 | CHECKING THE QUALITY | As per approved Pickling & Passivation Procedure |  | Pickling & Passivation Report | H |  | SW |  |  |  |  |  |  |  |  |  |
| 9.0 | Coating |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 9.1 | Blasting |  | As per approved procedure | Surface profile Measurement | Approved drawing & As per approved procedure |  | Inspection Report. | H |  | SW |  |  |  |  |  |  |  |  |  |
| 9.2 | Final paint, Visual & DFT |  | As per approved procedure | DFT Measurement | Approved drawing & As per approved procedure |  | Inspection Report. | H |  | SW |  |  |  |  |  |  |  |  |  |
| 10.0 | Identification marking & final inspection |  | Drawing | Visual | Drawing |  | Inspection Report | H |  | SW |  |  |  |  |  |  |  |  |  |
| 11.0 | IRC(Inspection release certificate) & Final Document |  | Approved Final Data Book Index | Fianl Data Book | Fianl Data Book |  | Fianl Data Book | H |  | H |  |  |  |  |  |  |  |  |  |